14. 	HSC EQUILIBRIUM MODULE SAMPLES

Contents of an Input File for GIBBS Program

§Copper Smelting at 1300 C			' Heading

1				' 0 = results to screen, 1= results to file

6   4   0   3   3   2   1    		' Elements, phases, inv. phases, and

' ^ number of components / phase 1., etc.

'N2(g)               '  2.00  0.00  0.00  0.00  0.00  0.00		' stoichiomet.

'O2(g)               '  0.00  2.00  0.00  0.00  0.00  0.00		' matrix

'SO2(g)              '  0.00  2.00  1.00  0.00  0.00  0.00

'*2FeO*SiO2(l)       '  0.00  4.00  0.00  2.00  1.00  0.00

'SiO2(l)             '  0.00  2.00  0.00  0.00  1.00  0.00

'Cu2O(l)             '  0.00  1.00  0.00  0.00  0.00  2.00

'Cu2S                '  0.00  0.00  1.00  0.00  0.00  2.00

'FeS                 '  0.00  0.00  1.00  1.00  0.00  0.00

'Cu                  '  0.00  0.00  0.00  0.00  0.00  1.00

4

1573.150				' Equilibrium temperature (K)

0.000000E+00  1.916105E+02  3		' H, S, number of temperature intervals

2.919177E+01 -1.121312E-03  0.000000E+00  4.091976E-06  0.000000E+00  0.000000E+00

400.000      0.000000E+00			' ^ A, B, C, D, E, F (J/(mol*K))

2.255176E+01  1.320889E-02  3.129632E+05 -3.389040E-06  0.000000E+00  0.000000E+00

1600.000      0.000000E+00			' Temperature (K), H (J/mol)

3.684012E+01  2.594080E-04 -5.478948E+06  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  2.051470E+02  1		' H (J/mol), S (J/(mol*K)), ()

3.132312E+01  3.893657E-03 -3.105337E+05 -3.349854E-07  0.000000E+00  0.000000E+00

-2.968130E+05  2.482210E+02  3

1.734500E+01  7.922700E-02  2.646000E+05 -4.563100E-05  0.000000E+00  0.000000E+00

700.000      0.000000E+00

5.164756E+01  6.297887E-03 -2.158751E+06 -1.367747E-06  0.000000E+00  0.000000E+00

2000.000      0.000000E+00

6.665800E+01 -4.478000E-03 -1.128930E+07  8.430000E-07  0.000000E+00  0.000000E+00

-1.458188E+06  9.729792E+01  1

2.405800E+02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-9.275245E+05  9.310607E+00  1

8.577200E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.302203E+05  9.640145E+01  1

9.991399E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-8.117000E+04  1.161520E+02  4

4.793800E+01  9.717300E-02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

376.000      3.619000E+03

1.184100E+02 -5.818200E-02  7.920001E+04  2.231700E-05  0.000000E+00  0.000000E+00

720.000      1.172000E+03

8.372372E+01 -1.253259E-03  2.450114E+05 -6.180060E-07  0.000000E+00  0.000000E+00

1400.000      1.284500E+04

8.966300E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.016710E+05  6.032100E+01  4

-2.732690E+02  7.791840E-01  8.124200E+06  0.000000E+00  0.000000E+00  0.000000E+00

411.000      1.665000E+03

7.235800E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

598.000      3.970000E+02

9.458400E+01 -8.366901E-02  1.411000E+05  4.794300E-05  0.000000E+00  0.000000E+00

1465.000      3.246400E+04

6.255100E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  3.316400E+01  2

4.057800E+01 -1.132500E-02 -3.284000E+05  9.800000E-06  0.000000E+00  0.000000E+00

1358.000      1.313800E+04

3.284400E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

5  1  2  5  7  8			' Raw materials, and their serial numbers

298.150    298.150    298.150    298.150    298.150

2				' ^ Temperatures of the raw materials (K)

13				' Number of equilibria to be calculated

3 3 3 2 2				' 2 = constant input amount, 3 = increases

1.0000000E-03 1.8850000E+00			' Amount of raw material 1., step (mol)

1.0000000E-03 5.0000000E-01			' Amount of raw material 2., step (mol)

1.0000000E-03 1.2500000E-01			' Amount of raw material 5., step (mol)

1.0000000E+00				' Amount of raw material 7. (mol)

2.0000000E+00				' Amount of raw material 8. (mol)

10				' Exit

' 9 = Activity Coefficients if values other than 1

Input File for SOLGASMIX Program (Amounts in moles)

§Copper Smelting at 1300 C			' Heading

0				' 0 = mole mode, 1= gram mode

6   4   1   3   3   2    			' Elements, phases, inv. phases, and

' ^ number of components / phase 1., etc.

'N2(g)               '  2.00  0.00  0.00  0.00  0.00  0.00		' stoichiomet.

'O2(g)               '  0.00  2.00  0.00  0.00  0.00  0.00		' matrix

'SO2(g)              '  0.00  2.00  1.00  0.00  0.00  0.00

'*2FeO*SiO2(l)       '  0.00  4.00  0.00  2.00  1.00  0.00

'SiO2(l)             '  0.00  2.00  0.00  0.00  1.00  0.00

'Cu2O(l)             '  0.00  1.00  0.00  0.00  0.00  2.00

'Cu2S                '  0.00  0.00  1.00  0.00  0.00  2.00

'FeS                 '  0.00  0.00  1.00  1.00  0.00  0.00

'Cu                  '  0.00  0.00  0.00  0.00  0.00  1.00

4

1573.150				' Equilibrium temperature (K)

0.000000E+00  1.916105E+02  3		' H, S, number of temperature intervals

2.919177E+01 -1.121312E-03  0.000000E+00  4.091976E-06  0.000000E+00  0.000000E+00

400.000      0.000000E+00			' ^ A, B, C, D, E, F (J/(mol*K))

2.255176E+01  1.320889E-02  3.129632E+05 -3.389040E-06  0.000000E+00  0.000000E+00

1600.000      0.000000E+00			' Temperature (K), H (J/mol)

3.684012E+01  2.594080E-04 -5.478948E+06  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  2.051470E+02  1		' H (J/mol), S (J/(mol*K)), ()

3.132312E+01  3.893657E-03 -3.105337E+05 -3.349854E-07  0.000000E+00  0.000000E+00

-2.968130E+05  2.482210E+02  3

1.734500E+01  7.922700E-02  2.646000E+05 -4.563100E-05  0.000000E+00  0.000000E+00

700.000      0.000000E+00

5.164756E+01  6.297887E-03 -2.158751E+06 -1.367747E-06  0.000000E+00  0.000000E+00

2000.000      0.000000E+00

6.665800E+01 -4.478000E-03 -1.128930E+07  8.430000E-07  0.000000E+00  0.000000E+00

-1.458188E+06  9.729792E+01  1

2.405800E+02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-9.275245E+05  9.310607E+00  1

8.577200E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.302203E+05  9.640145E+01  1

9.991399E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-8.117000E+04  1.161520E+02  4

4.793800E+01  9.717300E-02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

376.000      3.619000E+03

1.184100E+02 -5.818200E-02  7.920001E+04  2.231700E-05  0.000000E+00  0.000000E+00

720.000      1.172000E+03

8.372372E+01 -1.253259E-03  2.450114E+05 -6.180060E-07  0.000000E+00  0.000000E+00

1400.000      1.284500E+04

8.966300E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.016710E+05  6.032100E+01  4

-2.732690E+02  7.791840E-01  8.124200E+06  0.000000E+00  0.000000E+00  0.000000E+00

411.000      1.665000E+03

7.235800E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

598.000      3.970000E+02

9.458400E+01 -8.366901E-02  1.411000E+05  4.794300E-05  0.000000E+00  0.000000E+00

1465.000      3.246400E+04

6.255100E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  3.316400E+01  2

4.057800E+01 -1.132500E-02 -3.284000E+05  9.800000E-06  0.000000E+00  0.000000E+00

1358.000      1.313800E+04

3.284400E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

5  1  2  5  7  8  ' Raw materials, and their row numbers in the stoichiometry matrix

298.150    298.150    298.150    298.150    298.150

2				' ^ Temperatures of the raw materials (K)

13				' Number of equilibria to be calculated

3 3 3 2 2				' 2 = constant input amount, 3 = increases

1.0000000E-03 1.8850000E+00			' Amount of raw material 1., step (mol)

1.0000000E-03 5.0000000E-01			' Amount of raw material 2., step (mol)

1.0000000E-03 1.2500000E-01			' Amount of raw material 5., step (mol)

1.0000000E+00				' Amount of raw material 7. (mol)

2.0000000E+00				' Amount of raw material 8. (mol)

10				' Exit

Input File for SOLGASMIX (Input amounts in grams)

§Copper Smelting at 1300 C			' Heading

1				' 0 = mole mode, 1= gram mode

6   4   1   3   3   2  ' Elements, phases, inv. phases, and number of components / phase 1...

'N2(g)               '  2.00  0.00  0.00  0.00  0.00  0.00		' stoichiomet.

'O2(g)               '  0.00  2.00  0.00  0.00  0.00  0.00		' matrix

'SO2(g)              '  0.00  2.00  1.00  0.00  0.00  0.00

'*2FeO*SiO2(l)       '  0.00  4.00  0.00  2.00  1.00  0.00

'SiO2(l)             '  0.00  2.00  0.00  0.00  1.00  0.00

'Cu2O(l)             '  0.00  1.00  0.00  0.00  0.00  2.00

'Cu2S                '  0.00  0.00  1.00  0.00  0.00  2.00

'FeS                 '  0.00  0.00  1.00  1.00  0.00  0.00

'Cu                  '  0.00  0.00  0.00  0.00  0.00  1.00

14.007				' N Mol. Weight g/mol

15.999				' O

32.060				' S

55.847				' Fe

28.086				' Si

63.546				' Cu

4

1573.150				' Equilibrium temperature (K)

0.000000E+00  1.916105E+02  3		' H, S, number of temperature intervals

2.919177E+01 -1.121312E-03  0.000000E+00  4.091976E-06  0.000000E+00  0.000000E+00

400.000      0.000000E+00			' ^ A, B, C, D, E, F (J/(mol*K))

2.255176E+01  1.320889E-02  3.129632E+05 -3.389040E-06  0.000000E+00  0.000000E+00

1600.000      0.000000E+00			' Temperature (K), H (J/mol)

3.684012E+01  2.594080E-04 -5.478948E+06  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  2.051470E+02  1		' H (J/mol), S (J/(mol*K)), ()

3.132312E+01  3.893657E-03 -3.105337E+05 -3.349854E-07  0.000000E+00  0.000000E+00

-2.968130E+05  2.482210E+02  3

1.734500E+01  7.922700E-02  2.646000E+05 -4.563100E-05  0.000000E+00  0.000000E+00

700.000      0.000000E+00

5.164756E+01  6.297887E-03 -2.158751E+06 -1.367747E-06  0.000000E+00  0.000000E+00

2000.000      0.000000E+00

6.665800E+01 -4.478000E-03 -1.128930E+07  8.430000E-07  0.000000E+00  0.000000E+00

-1.458188E+06  9.729792E+01  1

2.405800E+02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-9.275245E+05  9.310607E+00  1

8.577200E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.302203E+05  9.640145E+01  1

9.991399E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-8.117000E+04  1.161520E+02  4

4.793800E+01  9.717300E-02  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

376.000      3.619000E+03

1.184100E+02 -5.818200E-02  7.920001E+04  2.231700E-05  0.000000E+00  0.000000E+00

720.000      1.172000E+03

8.372372E+01 -1.253259E-03  2.450114E+05 -6.180060E-07  0.000000E+00  0.000000E+00

1400.000      1.284500E+04

8.966300E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

-1.016710E+05  6.032100E+01  4

-2.732690E+02  7.791840E-01  8.124200E+06  0.000000E+00  0.000000E+00  0.000000E+00

411.000      1.665000E+03

7.235800E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

598.000      3.970000E+02

9.458400E+01 -8.366901E-02  1.411000E+05  4.794300E-05  0.000000E+00  0.000000E+00

1465.000      3.246400E+04

6.255100E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

0.000000E+00  3.316400E+01  2

4.057800E+01 -1.132500E-02 -3.284000E+05  9.800000E-06  0.000000E+00  0.000000E+00

1358.000      1.313800E+04

3.284400E+01  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00  0.000000E+00

5  1  2  5  7  8 	' Raw materials, and their row numbers in the stoichiometry matrix

298.150    298.150    298.150    298.150    298.150

2				' ^ Temperatures of the raw materials (K)

13				' Number of equilibria to be calculated

3 3 3 2 2				' 2 = constant input amount, 3 = increases

2.8013401E-02 5.2805256E+01			' Amount of raw material 1., step (g)

3.1998802E-02 1.5999400E+01			' Amount of raw material 2., step (g)

6.0084306E-02 7.5105376E+00			' Amount of raw material 5., step (g)

1.5915201E+02				' Amount of raw material 7. (g)

1.7581400E+02				' Amount of raw material 8. (g)

- ' Exit

Case 1: Hydration of Magnesia Chrome Bricks

Magnesia chrome bricks are widely used as a lining material in pyrometallurgical applications because of their stability in process conditions. However, at room temperatures they easily react with moisture and crumble due to hydration reactions. HSC software can be used to estimate the lowest temperature, which must be exceeded to prevent such reactions and to specify these reactions.

Magnesia chrome bricks contain magnesium, chromium, iron and oxygen. All species, which contain these elements and hydrogen, can easily be collected to the Equilibrium module from the database. The following ideas were used to specify the system (see Fig 2):

-	Metallic substances were removed, as they are not needed in these conditions.

-	Gas species (16) were inserted in the gas phase.

-	Other species (25) were assumed to exist as pure substances (invariant phases), because of the low temperatures where molten mixtures do not exist.

-	MgO, Cr2O3 and Fe2O3 raw materials were added according to their amount in the brick: MgO 60, Cr2O3 18 and Fe2O3 14 kg.

-	Water gas was added to the gas phase. The amount was set slightly higher than needed to hydrate all species in the brick.

-	A small amount of nitrogen was added to the gas phase.

The results of the calculations are shown in Fig. 1. This diagram shows that hydration of the bricks is possible if the temperature of the lining is lower than 270 °C. Hydration damage is caused only due to the formation of magnesium hydroxide; the chromium and iron do not take part in hydration reactions. Magnesium oxide (periclase) forms the matrix of the brick, therefore hydration of magnesium oxide crumbles the whole construction.

Figure 1. Calculation results for hydration of magnesia chrome brick.

Figure 2. Specification of phases and species in the Magnesia Chrome brick example.

Case 2: Ammonia Synthesis (by Panu Talonen)

Ammonia was expensive to produce before the current process, which uses high pressure and iron catalyst, was invented. The synthesis is usually made at temperature of 370 – 540 °C. The effect of pressure on the ammonia formation can easily be evaluated with HSC Equilibrium module. The formation reaction can be written as follows:

N2(g) + 3 H2(g) -> 2NH3(g)

The number of gas moles decreases in this reaction and therefore high pressure may be assumed to favor the synthesis. The equilibrium calculation may be carried out as described in Chapter 13. The chemical system specification and other calculation parameters are shown in Fig. 2. The calculations are carried out by increasing the pressure from 0.001 to 1000 bar at a constant temperature of 480 °C.

The calculated results are shown in Fig. 3. It is easy to see that at normal 1 bar pressure it is quite impossible to produce high amounts of ammonia. It also seems that synthesis should be done at the highest possible pressure. However, modern ammonia plants operate at about 150 bar pressure for economic reasons. The ammonia is condensed from the gas mixture and the unreacted hydrogen and nitrogen are recycled back to the reactor.

Figure 3. Calculation results for ammonia synthesis example.

Figure 4. Specification of phases and species in ammonia synthesis example.

Case 3: Decomposition of MgCl2*6H2O

All compounds will decompose if the temperature is high enough. Especially substances with combined water will decompose at quite low temperatures. The decomposition temperatures may be found from many different handbooks, but they may also be calculated with the HSC Equilibrium module if the basic data is available in the HSC database. Magnesium chloride forms a MgCl2*6H2O compound which decomposes according to the reaction:

MgCl2*6H2O -> MgCl2*4H2O + 2H2O(g)

MgCl2*4H2O -> MgCl2*2H2O + 2H2O(g), etc.

The decomposition temperature as well as the decomposition vapor pressure may be calculated using the chemical system specification shown in Fig. 5. The user must specify all possible condensed phases as well as a gas phase. Please note: A) Small nitrogen amount stabilize the gas phase, B) small Cl2(g) and O2(g) amounts shift the material balance out from stoichiometric one and C) Mg(g) allows magnesium to enter the gas phase also.

The results of the calculations are shown in Figs. 6 and 7. The decomposition seems to start at 100 °C, see Fig. 6. The vapor composition is drawn in Fig. 7 by selecting the Equilibrium Composition option. This diagram shows that the vapor pressure of water is 0.67 bar at 175 °C and 1 bar total pressure. To calculate vapor pressure at higher temperatures, the total pressure must be increased, for example, to 10 bar.

Figure 5. Specification of phases and species in MgCl2*6H2O example.

Figure 6. Calculation results for MgCl2*6H2O decomposition example.

Figure 7. Vapor composition at a total pressure of 1 bar.

Case 4: Decomposition of FeSO4*7H2O (by Ben Karlemo)

Thermal decomposition of a chemical compound will sometimes give valuable information of its behaviour in a real chemical process. This evaluation may be carried out with the HSC Equilibrium module and with a thermo-gravimetric analyzer. These evaluations have been made in this example for FeSO4*7H2O. The chemical system specifications for the HSC equilibrium module are shown in Fig. 8. Please note (see Chapter 13.4): A) The small amount of nitrogen stabilizes the gas phase, B) the small amount 1E-5 kmol of O2(g) shifts the material balance away from the stoichiometric one, C) Fe(g) allows iron to enter the gas phase also, and D) Solgasmix routine has been used. The results are shown in Fig. 9.

The hydrates gradually decompose at 50 to 200 °C and sulfates at 400 to 650 °C. Hematite will reduce to magnetite at 1250 °C. These results may be used to explain the experimental thermo-gravimetric results shown in Fig. 10. The TG curve shows the actual weight change and the DSC curve shows the enthalpy change compared to the reference test.

Figure 8. The specification of phases and species for the equilibrium calculations.

Figure 9. The result of the calculated decomposition of FeSO4*7H2O.

The theoretical and experimental weight change curves are compared in Fig. 11, which is calculated in MS Excel. Both curves are in quite good correlation with each other. The decomposition occurs at slightly higher temperatures in the experimental results than in the calculated ones, but this may be explained by some kinetic effects. The final weight of the sample was nearly the same in the experimental and theoretical results at high temperatures. The decomposition reactions may also be verified by comparing the analyzed and the calculated gas composition with each other.

Figure 10. Results of FeSO4*7H2O run on NETSCH TG-DSC analyzer under nitrogen atmosphere showing TG and DSC curves. Heating rate was 5 °C/min.

Figure 11. The comparison of the measured and calculated mass change of FeSO4*7H2O.

Case 5: Alkali circulation in Blast Furnace (by Riku Sarkkinen)

Alkali metals tend to enrich in the iron blast furnace. The alkali content in raw materials (pellets, sinter and coke) is not so high, but they evaporate at the bottom part of the furnace (~1500 °C) and do not exit with the products (slag, iron) easily. Neither do they exit with the process gas, which goes upward, because the temperature is quite low at the top of the furnace (~100 °C). This problem may be evaluated with the HSC Equilibrium module.

The chemical system specification is shown in Fig. 13. The raw material amounts are based on the following assumptions: Coke ash analysis (main components): SiO2 53, CaO 3, MgO 2, and Al2O3 27 wt %. Process gas is formed by air reaction with coke, the main components in the gas phase are CO(g), CO2(g) and N2(g). The alkali elements are K and Na. The calculations are carried out as described in Chapter 13 by increasing the temperature from 500 to 2000 °C. Iron has not been taken into account because the alkali circulation occurs above the liquid iron zone. Equilibrium calculations were made as described in Chapter 13.

The calculation results are shown in Fig. 12. At high temperatures almost all the sodium and most of the potassium seems to be in elemental form in the gas phase. These gas species flow with the main process gases upward where cold charge materials decrease the temperature and alkalis react with the slag components. The reaction products are mainly sodium and potassium carbonates, sodium silicates and potassium alumina silicates. These solid compounds flow downwards with the blast furnace charge materials to the high temperature zone at the bottom of the furnace, where the alkali components vaporize again, which leads to the alkali circulation.

Figure 12. Equilibrium results of alkalis and slag components as a function of temperature.

Figure 13. Specification of phases and species in the Blast Furnace example.